Sodium  Formate  Analysis  Report

| No. | 2009-09-05 | Quantity | 500MT |
| --- | --- | --- | --- |
| Quality Standard | GB/T6009-2003 | Analysis Date | 2009-09-05 |
| Item | Value | Analysis Result |
|  | First Grade of I Type |  |
| HCOO Na %≥ | 98.0 | 98.02 |
| Water %≤ | 1.00 | 0.82 |
| NAOH %≤ | 0.50 | 0.46 |
| NaCL %≤ | 0.20 | 0.23 |
| Na2C0 %≤ | 0.50 | 0.449 |
| Na2S %≤ | 0.03 | 0.021 |
| Conclusion | First Grade of I Type |
| Note |  |
| Check | Haoyi Xu | Test | Yun Li |